## Slide 1
Unit 3: Equilibrium Carrier Concentrations
Lecture 3.1:
The Fermi function

## Slide 2: Occupation of states
The topic of Unit 3 is understanding how we compute the equilibrium concentrations of electrons and holes in semiconductors. Our first step towards doing that is to understand a quantity known as the Fermi function.
Here is the dividing line between the filled states and the empty states. That line will turn out to be very useful to us in semiconductors.

## Slide 3: Fermi level
we can draw a line and that line we're going to call the Fermi level below that line the states will be mostly filled. Above that line, the states will be mostly empty
there is a very simple equation that
describes the probability the state at any energy is occupied by an electron. That simple equation is the Fermi function

## Slide 4: The Fermi function

## Slide 5: More about the Fermi function
What we'll find is that the width of that transition is determined by the temperature.

## Slide 6: Effect of temperature
If the temperature increase, the width of the transition from high probability of being occupied to low probability of being occupied gets broader. As the semiconductor cool down, the width of that region gets sharper.

## Slide 7: Electrons and holes
Given a semiconductor, where is the Fermi level?

## Slide 8: Conduction band
now let's apply this Fermi function to the conduction band.
A nondegenerate n-type semiconductor is one in which the states have a small probability of being filled.

## Slide 9: Valence band
A nondegenerate p-type semiconductor, there will be a small probability that the states are empty in the valence band.

## Slide 10: Nondegenerate semiconductors
In other words, a nondegenerate semiconductor is one in which the states in the conduction band are always well above the Fermi energy, and the states in the valence band are well below the Fermi energy

## Slide 11: Energy band diagram of an intrinsic semiconductor
It turns out it's not exactly in the middle. We'll see why later, but that's because the density of states in the valence band is slightly different from the density of states in the conduction band.

## Slide 12: Energy band diagram and carrier densities

## Slide 13: Summary
The Fermi function gives the probability that a state (if it exists) is occupied in equilibrium.
The two key parameters in the Fermi function are the Fermi level and the temperature.

## Slide 14
Unit 3: Equilibrium Carrier Concentrations
Lecture 3.2:
Fermi-Dirac integrals

## Slide 15: The Fermi function
The Fermi function gives the probability that a state (if it exists) is occupied in equilibrium.
The two key parameters in the Fermi function are the Fermi level and the temperature.
The reason we need to understand the Fermi function is because it is used to compute carrier densities in semi-conductors

## Slide 16: Equilibrium carrier densities
So our goal is to understand what the carrier density is in the conduction band, and what the hole density is in the valence band given a particular location of this Fermi energy

## Slide 17: Two options
Our goal is to relate the carrier density to the Fermi level and to the properties of the semiconductor.
We can do the calculation two ways:
  1) In k-space
  2) In energy space

## Slide 18: 3D bulk semiconductor: k-space

## Slide 19: Density-of-states in k-space

## Slide 20: Energy space (parabolic bands)
Let's do the calculation in 3D

## Slide 21: Distribution of electrons in the conduction band

## Slide 22: Distribution of electrons in the conduction band

## Slide 23: Compute the electron density
I can see that the result is going to depend on Fermi level and temperature. Because those two parameters are in the Fermi function. The result is also going to depend on the effective mass of the semiconductor and the number of equivalent valleys because those quantities are in the density of states.

## Slide 24: Energy space (3D)
A couple of definitions
That integral cannot be done analytically. It has to be done numerically!. The integral is called a Fermi-Dirac integral of order 1/2

## Slide 25: Fermi-Dirac integrals
In a nondegenerate semiconductor this complicated Fermi-Dirac integral reduces to the familiar exponential.

## Slide 26: Fermi-Dirac integral of order 1/2

## Slide 27: Nondegenerate semiconductor

## Slide 28: Compute the electron density

## Slide 29: Compute the hole density

## Slide 30: Summary

## Slide 31
Unit 3: Equilibrium Carrier Concentrations
Lecture 3.3:
Carrier concentration
vs. Fermi level

## Slide 32: Carrier concentrations

## Slide 33: Electron concentration

## Slide 34: Hole concentration

## Slide 35: Fermi level and electron concentration

## Slide 36: Fermi level and hole concentration

## Slide 37: From carrier concentration to Fermi level
So we can go either way. Given n, we can compute EF. Given EF, we can compute n.

## Slide 38: np product
The equilibrium product of the electron and hole concentrations is a very important quantity for a semiconductor.

## Slide 39: np product
ni doesn't depend on the Fermi level, so it's valid in an intrinsic semiconductor or any semiconductor.

## Slide 40: np product
The wider the band gap, the harder it is to break those covalent bonds. The higher the temperature, the easier it is for the thermal energy to break those covalent bonds

## Slide 41: Recall: Fermi level and hole concentration

## Slide 42: Another way
Now we have another way to do this problem
ni is difficult to compute exactly! because it depends exponentially on band gap and temperature

## Slide 43: E-band diagram for N-type semiconductor

## Slide 44: E-band diagram for P-type semiconductor

## Slide 45: Intrinsic semiconductor

## Slide 46: The intrinsic Fermi level
We will call the Fermi level in the intrinsic condition Ei instead of EF.

## Slide 47: The intrinsic level: Silicon
let's work out some numbers for silicon

## Slide 48: Alternative expression for carrier densities
These two relations relate the carrier densities to the Fermi level and they're perfectly adequate. But there's another way to do this that's commonly done and it is useful also.
These two expressions are equal.

## Slide 49: “Reading” an E-band diagram

## Slide 50: Summary

## Slide 51
Unit 3: Equilibrium Carrier Concentrations
Lecture 3.4:
Carrier concentration
vs. doping density

## Slide 52: Carrier concentrations vs. Fermi level

## Slide 53: Space charge density

## Slide 54: Space charge neutrality
Nature abhors a charge.
Mobile charges (electrons and holes) will be attracted to the immobile ionized dopants), so that the net charge is zero.
Almost uniform semiconductors will be nearly neutral, but with strong non-uniformities (e.g. PN junctions), there will be a space charge.

## Slide 55: Fully ionized dopants

## Slide 56: Space charge neutrality again

## Slide 57: Solving for the carrier density

## Slide 58: Result: N-type

## Slide 59: Result: P-type

## Slide 60: Example 1

## Slide 61: Soln

## Slide 62: Example 2

## Slide 63: Soln

## Slide 64: Conclusion

## Slide 65: Summary

## Slide 66
Unit 3: Equilibrium Carrier Concentrations
Lecture 3.5:
Carrier concentration
vs. temperature

## Slide 67: Carrier concentration vs. temperature
How the carrier concentration varies with temperature?

## Slide 68: The extrinsic region

## Slide 69: The extrinsic region

## Slide 70: The intrinsic region

## Slide 71: Result: N-type

## Slide 72: Result: P-type

## Slide 73: Example 3

## Slide 74: Soln

## Slide 75: Soln

## Slide 76: Comment

## Slide 77: The freeze-out region
Net doping density >> intrinsic concentration

## Slide 78: Solving for the carrier density: N-type

## Slide 79: Low temperature

## Slide 80: Ionized donor concentration

## Slide 81: Ionized donor concentration

## Slide 82: Ionized dopant concentration

## Slide 83: Example: N-type sample

## Slide 84: The freeze-out region

## Slide 85: The freeze-out region

## Slide 86: Comment

## Slide 87: Metal-insulator transition

## Slide 88: Question
We now understand how the carrier concentration varies with temperature. How does the Fermi level vary with temperature?

## Slide 89: Fermi level vs. temperature

## Slide 90: Summary

## Slide 91
Unit 3: Equilibrium Carrier Concentrations
Lecture 3.6:
Unit 3 Summary

## Slide 92: Fermi function
The Fermi function gives the probability that a state (if it exists) is occupied in equilibrium.
The two key parameters in the Fermi function are the Fermi level and the temperature.

## Slide 93: Fermi level and temperature

## Slide 94: Distribution of carriers in the bands

## Slide 95: Fermi-Dirac integrals

## Slide 96: FD integrals and exponentials

## Slide 97: Nondegenerate semiconductors

## Slide 98: Carrier densities for nondegenerate semiconductors

## Slide 99: np product

## Slide 100: The intrinsic Fermi level

## Slide 101: Carrier concentration relations (nondegenerate)

## Slide 102: Reading an e-band diagram

## Slide 103: Carrier concentration vs. doping

## Slide 104: Extrinsic region

## Slide 105: The intrinsic region

## Slide 106: The freeze out region (just for your information)

## Slide 107: Fermi level vs. temperature

## Slide 108: Unit summary