## Slide 1
Unit 4: Carrier Transport,
Recombination, and Generation

## Slide 2
Unit 4 is all about how charge carriers, electrons, and holes respond out of equilibrium under the normal operating conditions of a semiconductor device.

## Slide 3: Semiconductor in equilibrium
This slab is just sitting there in equilibrium. But thermal energy is rattling the atoms around. The atoms are interacting with the electrons and knocking them around. So these electrons are in random, thermal, chaotic motion.Their overall average velocity is zero.

## Slide 4: Semiconductor under bias
The average drift velocity is proportional to the electric field. The constant of proportionality is the mobility

## Slide 5: Drift current and drift velocity

## Slide 6: Velocity and electric field
When you measure in the lab the average velocity versus electric field of electrons, and holes, in bulk semiconductor. The characteristic will look something like this
If you apply large voltages, we can see that the current doesn't increase indefinitely. The velocity doesn't increase indefinitely. It tends to saturate at a value.

## Slide 7: Velocity vs. electric field
In almost any semiconductor, you will find that under high electric fields, the velocity is reduced to on the order of 10 to the 7th centimeters per second. That's sort of the speed limit for electrons and holes in bulk semiconductors

## Slide 8: Drift current

## Slide 9: Mobility vs. doping
As long as we're in the low-field regime, the mobility is simply a material-dependent quantity, tightly related to the scattering.
Why is the mobility getting lower and lower? Well, the reason has to do with increased scattering.

## Slide 10: Ionized impurity scattering
That will reduce the
velocity of the electrons in one particular direction, and lower the mobility.

## Slide 11: Mobility vs. temperature
At high temperatures, there's much more random, thermal motion of the lattice jiggling around. That lattice interacts with electrons and knocks electrons around more rigorously. The time between scattering events drops, the mean free path drops, and the mobility drops the higher the temperature is due to that process
As the temperature increase , the average thermal velocity increase . So, electrons zip past these charged, ionized impurities faster. They interact less.They're scattered less. So, the mobility gets higher

## Slide 12: Comment
If we're working with semiconductor devices, we will undoubtedly need to know the mobility. In order to understand what the mobility is or to look it up in a table, we need to know what the doping is and we need to know what the temperature is

## Slide 13: Drift current, conductivity, resistivity
Conductivity =
Resistivity=

## Slide 14: Resistance

## Slide 15: Fick’s Law of diffusion
There is no actual force that's pushing the holes in this case from high concentration to low concentration. It's simply a statistical effect.

## Slide 16: Diffusion currents

## Slide 17: Nonuniformly doped semiconductor in equilibrium

## Slide 18: Summary: Drift- diffusion equation

## Slide 19
Unit 4: Carrier Transport,
Recombination, and Generation
Lecture 4.4:
Carrier recombination

## Slide 20: Equilibrium and non-equilibrium

## Slide 21: Carrier recombination
intuitively, if we perturb a system, we expect the system to respond by trying to return to equilibrium. And oftentimes, this return to equilibrium is an exponential process.

## Slide 22: How can excess carriers recombine?
We will discuss three different ways:
  1) Band-to-band (radiative) recombination
  2) Auger recombination
  3) SRH (defect-assisted) recombination
There are three different important and common ways that this recombination can occur

## Slide 23: 1) Band-to-band (radiative) recombination
The change is negative because it's reducing their concentration.

## Slide 24: Low level injection
The term “low level injection” means that the excess carrier concentration is orders of magnitude smaller than the equilibrium majority carrier concentration but orders of magnitude larger that the equilibrium minority carrier concentration.

## Slide 25: Example: Low level injection in a p-type semiconductor
Low level injection has negligible influence on the majority carriers. It has a huge influence on the minority carriers.

## Slide 26: Low level injection in a p-type semi
It's a characteristic time for this recombination process.

## Slide 27: Excess carrier concentration vs. time

## Slide 28: 2) Auger recombination
If it's an n-type semiconductor there are a lot of electrons nearby. They might give up the energy to a nearby electron and kick it way up in the conduction band.

## Slide 29: Low level injection in an n-type semiconductor
Auger recombination time

## Slide 30: 3) SRH (defect-assisted) recombination
The current can't flow through these defects. But these defects can mediate recombination processes.
The statistics of this recombination process are described by this equation.
concentration of traps= N sub T.

## Slide 31: Low level injection in a p-type semiconductor

## Slide 32: Recombination under low level injection

## Slide 33: Multiple recombination processes

## Slide 34: Discussion

## Slide 35: BB recombination in direct gap semiconductors

## Slide 36: BB recombination in indirect gap semiconductors
to find the right lattice vibration with the right momentum to facilitate this process is going to be harder to do.

## Slide 37: Three type of recombination

## Slide 38: Recombination-generation

## Slide 39: 3) SRH (defect-assisted) generation

## Slide 40: Summary

## Slide 41
Unit 4: Carrier Transport,
Recombination, and Generation
Lecture 4.5:
Carrier generation

## Slide 42: Recombination

## Slide 43: Photoelectric effect (optical generation)
If the energy of the photons is above the work function of a metal, then we can eject electrons out of this potential well that holds them in the metal into the vacuum and detect the current. This is called the photoelectric effect

## Slide 44: Optical generation in semiconductors
This is just an equivalent way of expressing energy in terms of wavelength

## Slide 45: Carrier generation from a solar spectrum
The wavelengths that are less than 1.13 micrometers, those photons have enough energy to create electron-hole pairs.

## Slide 46: Thermalization
That extra energy will be shed by various scattering processes. And in a few, probably tens of femtoseconds, the electrons will end up down at the bottom

## Slide 47: Thermalization on an E(k) diagram

## Slide 48: Thermalization on an E(k) diagram
excess energy then during the thermalization process would typically be released as heat. And that's an undesirable side-effect of this process. It's energy that is just wasted.

## Slide 49: Optical absorption in a direct gap semiconductor
Now that process needs to conserve energy and momentum!

## Slide 50: Optical absorption in an indirect gap semiconductor
Energy and momentum must still be conserved, but in order to do this, we're going to need a lattice vibration.
because now we need to find a phonon,
a lattice vibration, with a proper momentum to facilitate the transition. So that's a less probable event.

## Slide 51: Optical absorption vs. semiconductor thickness

## Slide 52: Absorption coefficient
That flux will be absorbed as it penetrates into the semiconductor. And it will be absorbed through this expression. Where x is the depth into the semiconductor and Alpha is the absorption coefficient
We simply differentiate this position-dependent flux, and the expression gives us the generation rate of electrons and hole pairs
So alpha is an important parameter. It's very strong in direct gap semiconductors. It's much weaker in indirect gap semiconductors

## Slide 53: Types of generation

## Slide 54: Impact ionization
Now as the energy continues to increase, the electron might gain so much energy that it has more energy than the band gap, and it can break the covalent bond, and a collision can occur with the lattice, and it can create an electron hole pair.

## Slide 55: Impact ionization: E(k) picture

## Slide 56: Impact ionization

## Slide 57: Generation

## Slide 58
Unit 4: Carrier Transport,
Recombination, and Generation
Lecture 4.6:
Unit 4 Summery

## Slide 59: Drift-diffusion equation
There's a component that we call the drift component due to the force an electric field exerts on carriers that pushes them along. And there is a component due to the diffusion of free carriers, electrons or holes, down a concentration gradient.
The mobility tells us how fast the carriers move in an electric field, and the diffusion coefficient tells us how quickly the carriers diffuse down a concentration gradient.

## Slide 60: Drift-diffusion equation

## Slide 61: Drift-diffusion equation

## Slide 62: Recombination

## Slide 63: Recombination processes

## Slide 64: Generation processes

## Slide 65: Unit 4 summary