## Slide 1
Unit 5: The Semiconductor Equations
Lecture 5.1: Mathematical formulation

## Slide 2: Solving semiconductor problems
(we may be out of equilibrium!)

## Slide 3: Equilibrium vs. non-equilibrium

## Slide 4: The unknowns
The three unknowns are the two quasi Fermi levels and the electrostatic potential. We need three equations in three unknowns

## Slide 5: First equation: Continuity equation for holes
The first equation is an equation for the hole density.
divergence of that flux physically represents a net flow out minus divergence represents a net flow in.

## Slide 6: One equation in 3 unknowns

## Slide 7: Gauss’s Law
In a semiconductor not in a vacuum, we will have the material will respond and polarize, and the permittivity of free space needs to be replaced by the relative dielectric constant of the semiconductor times epsilon sub 0.

## Slide 8: Gauss’s Law in 1D

## Slide 9: The Poisson equation

## Slide 10: The “semiconductor equations”
These are sometimes called the semiconductor equations because they're often taken as the fundamental description of any semiconductor device.
If we simply solve these for a semiconductor device, we can understand the operation of the semiconductor device.

## Slide 11: Semiconductor equations
These are three coupled, partial differential equations, they're non-linear, so their solution is not completely trivial,

## Slide 12: Discussion: Equilibrium

## Slide 13: Reminder: Generation and recombination

## Slide 14: Discussion

## Slide 15
The product of n and p is some material and temperature dependent parameter, this is what we call the intrinsic carrier concentration squared

## Slide 16: Summary: The semiconductor equations

## Slide 17
Unit 5: The Semiconductor Equations
Lecture 5.2:
Energy band diagrams

## Slide 18
In this unit we discuss very powerful qualitative way that will provide us with insightful, qualitative solutions to the semiconductor equations without doing any mathematics whatsoever.

## Slide 19: The semiconductor equations

## Slide 20: Energy band diagrams
An energy band diagram is a plot of the bottom of the conduction band and the top of the valence band vs. position.
Energy band diagrams are a powerful tool for understanding semiconductor devices because they provide qualitative solutions to the semiconductor equations.

## Slide 21: An important principle (in equilibrium)

## Slide 22: The Fermi level in equilibrium

## Slide 23: Band bending

## Slide 24: Voltage and electron potential energy

## Slide 25: Electrostatic potential vs. position

## Slide 26: Electrostatic potential causes band bending

## Slide 27: Band diagrams

## Slide 28: Practice

## Slide 29: Another example: NP junction in equilibrium

## Slide 30: Procedure: Equilibrium energy band diagram

## Slide 31: Energy band diagram

## Slide 32: Now, “read” the e-band diagram

## Slide 33: Electrostatic potential?

## Slide 34: Electrostatics: V(x)

## Slide 35: Electric field?

## Slide 36: Electric field: E (x)

## Slide 37: Carrier densities?

## Slide 38: Carrier densities vs. x

## Slide 39: Space charge?

## Slide 40: Electrostatics: rho(x)

## Slide 41: NP junction electrostatics

## Slide 42: More practice

## Slide 43: Where does the electric-field come from?

## Slide 44: Summary

## Slide 45
Unit 5: The Semiconductor Equations
Lecture 5.3:
Quasi-Fermi levels

## Slide 46: Equilibrium vs. non-equilibrium

## Slide 47: The semiconductor equations

## Slide 48: Where is the Fermi level?

## Slide 49: Now where is the Fermi level?
Same # of electrons, more holes -> need 2 Fermi levels!

## Slide 50: Quasi-Fermi levels

## Slide 51: Non-equilibrium

## Slide 52: NP product

## Slide 53: Some numbers (equilibrium)

## Slide 54: Some numbers (LL injection)

## Slide 55: Discussion

## Slide 56: E-band diagram of an N-type resistor

## Slide 57: Assumptions

## Slide 58: Summary

## Slide 59
Unit 5: The Semiconductor Equations
Lecture 5.4:
Minority carrier diffusion equation

## Slide 60
There are sort of two broad classes of semiconductor devices. There's one class that relies on minority carriers for their operation. Some examples would be solar cells or bipolar transistors. There are other devices that do not rely on the operation of excess carriers, which, there may be no excess carriers present, even under non-equilibrium conditions. example just a simple n-type resistor with two ideal contacts on it.
In this lecture, we're going to focus on minority carriers and show how we can mathematically solve the semiconductor equations analytically, relatively simply, by making suitable approximations for minority carrier devices.

## Slide 61: Semiconductor equations

## Slide 62: Solving the semiconductor equations
In order to solve them we basically
have three options:

## Slide 63: Outline of the lecture

## Slide 64: Minority carrier diffusion equation

## Slide 65: Minority carrier diffusion equation

## Slide 66: Reminder: Low level injection

## Slide 67: Example: MCDE for electrons in Si
Okay, so now we're going to go ahead and solve this problem with these numerical parameters under a number of different situations.

## Slide 68: Example 1: Steady-state, uniform illumination

## Slide 69: Example 1: Solution

## Slide 70: Example 1: Equilibrium Fermi level

## Slide 71: Example 1: Quasi-Fermi levels

## Slide 72: Example 2: Transient decay to equilibrium

## Slide 73: Example 2: Solution

## Slide 74: Example 2: Solution

## Slide 75: Example 2: Solution

## Slide 76: Example 3: SS diffusion in a long sample

## Slide 77: Example 3: Continued

## Slide 78: Example 3: Solution

## Slide 79: Example 4: SS diffusion in a short sample

## Slide 80: Example 4: Continued

## Slide 81: Example 4: Solution

## Slide 82: Example 5

## Slide 83: Example 5: Solution

## Slide 84: Example 5: Solution

## Slide 85: Example 6:

## Slide 86: Example 6: Solution

## Slide 87: Example 6: Energy band diagram
Now, there's a gradient of the quasi Fermi level here. That means there's an electron current in this problem. That represents the flow of electrons to the surface as they recombine and continue to, they're generated in the bulk, they diffuse to the surface, and continually recombine under these steady state conditions. That gives us a current towards the surface.

## Slide 88: Summary (i)

## Slide 89: Summary (ii)